## Slide 1
Matrix Evolve Workshop
Rotopol 2025
Dharana Jayawardane
Technical Manager

## Slide 2
  Reducing surface tension between molten polymer particles
  Acts on the sintering phase of the process
  Does not influence the viscosity (MFI) of a polymer
  Leaves the final properties of material unchanged
EVOLVE®

## Slide 3
  10-20% reduction in overall cycle time
  potentially increase production output
  Energy savings by 10-20% reduction in gas consumption
  Lower CO2 emission
  Reduction in the number of pinholes, leading to improved part quality
EVOLVE® - Benefits

## Slide 4
  Revolve® N-307 (MFI 3.5 / 0.939 g/cm3)
  Hexagonal 18-liter bin
  Ferry RS1.90 gas-powered oven
  Fixed Oven Temperature
  Varied Oven Time
  Optimum Condition achieved by assessing:
  Part Density
  Impact Strength (ARM-I Standard)
Experimental Study

## Slide 5
From Heat to Shape: The Journey of Polymer Transformation
Oven is heated up
Mould is taking in energy
Energy is transferred to the powder
Powder starts to melt
Powder to coalesce, sinter, densify
Cooling stage, Crystallization
Demoulding

## Slide 7
ARM Impact test
  Plaques conditioned at -40C
  Dart of 4.5 kg for 3 mm plaques
  Dart height is increased until failure
  Failure height and mode are recorded

## Slide 8
Ductile Vs Brittleness – Failure mode

## Slide 9
Chart: cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24
Impact Strength (J) | 0 | 59.09 | 76.22 | 65 | 73.3 | 65.8 | 74.4 | 79.7 | 88.6 | 99.9 | 104.7 | 97.5 | 102.1 | 0
Brittleness (%) | 100 | 100 | 33 | 33 | 23 | 28 | 25 | 0 | 0 | 0 | 0 | 0 | 0 | 100 | 100 | 100 | 100
Operating window
Operating window

## Slide 10
Part Density
  Plaques conditioned at room temperature
  Water bath
  Moulded part is weighed and then submerged into solution
  Very quick and easy method of understanding undercured material and high crystallinity

## Slide 11
Part Density vs. Cycle Time
Chart: Cook time (min)
| 9 | 10 | 11 | 12 | 13 | 14 | 16 | 18 | 20 | 21
N-307 | 0.9235 | 0.9244 | 0.9263 | 0.9314 | 0.937 | 0.94 | 0.941 | 0.941 | 0.9415 | 0.941

## Slide 12
PINHOLES-FREE
PINHOLES
Chart: Cook time (min)
| 9 | 10 | 11 | 12 | 13 | 14 | 16 | 18 | 20 | 21
N-307 | 0.9235 | 0.9244 | 0.9263 | 0.9314 | 0.937 | 0.94 | 0.941 | 0.941 | 0.9415 | 0.941
Part Density vs. Cycle Time

## Slide 13
Surface Pinholes
Processing conditions
Rotomoulding Tool surface
Powder quality

## Slide 14
Chart: Cook time (min)
| 9 | 10 | 11 | 12 | 13 | 14 | 16 | 18 | 20 | 21
N-307 | 0.9235 | 0.9244 | 0.9263 | 0.9314 | 0.937 | 0.94 | 0.941 | 0.941 | 0.9415 | 0.941
Evolve N-307 | 0.9267 | 0.9324 | 0.939 | 0.9423 | 0.9422 | 0.9425 | 0.9425 | 0.9426 | 0.9426 | 0.9428
Part Density vs. Cycle Time

## Slide 15
Chart: Cook time (min)
| 9 | 10 | 11 | 12 | 13 | 14 | 16 | 18 | 20 | 21
N-307 | 0.9235 | 0.9244 | 0.9263 | 0.9314 | 0.937 | 0.94 | 0.941 | 0.941 | 0.9415 | 0.941
Evolve N-307 | 0.9267 | 0.9324 | 0.939 | 0.9423 | 0.9422 | 0.9425 | 0.9425 | 0.9426 | 0.9426 | 0.9428
Part Density vs. Cycle Time

## Slide 16
Gas Consumption – Part Density
PIAT (°C) | REVOLVE N-307 | EVOLVE N-307 | GAS (M³)
120 | - | - | 0,64
148 | 0,9276 | 0,9332 | 1,58
159 | 0,9271 | 0,9345 | 1,72
172 | 0,9286 | 0,9372 | 1,93
185 | 0,9361 | 0,9389 | 2,37
190 | 0,9370 | 0,9401 | 2,81
210 | 0,9392 | 0,9410 | 3,25
25% less gas at same part density

## Slide 17
Chart: part density vs. Oven temperature
| 185 | 200 | 215 | 230 | 245 | 260 | 275
N-307 | 0.9276 | 0.929 | 0.931 | 0.936 | 0.937 | 0.939 | 0.9395
Evolve N-307 | 0.9332 | 0.9345 | 0.9372 | 0.9389 | 0.94 | 0.941 | 0.942
Energy Savings
Part Density vs. Oven Temperature

## Slide 18
Chart: part density vs. Oven temperature
| 185 | 200 | 215 | 230 | 245 | 260 | 275
N-307 | 0.9276 | 0.929 | 0.931 | 0.936 | 0.937 | 0.939 | 0.9395
Evolve N-307 | 0.9332 | 0.9345 | 0.9372 | 0.9389 | 0.94 | 0.941 | 0.942
Energy Savings
Part Density vs. Oven Temperature
ΔT

## Slide 19
Chart: Part Density vs. PIAT
| 148 | 159 | 172 | 185 | 190 | 210 | 220
N-307 | 0.9276 | 0.929 | 0.931 | 0.936 | 0.937 | 0.939 | 0.9395
Evolve N-307 | 0.9332 | 0.9345 | 0.9372 | 0.9389 | 0.94 | 0.941 | 0.942
Energy Savings
Part Density vs. Oven Temperature

## Slide 20
Chart: Part Density vs. PIAT
| 148 | 159 | 172 | 185 | 190 | 210 | 220
N-307 | 0.9276 | 0.929 | 0.931 | 0.936 | 0.937 | 0.939 | 0.9395
Evolve N-307 | 0.9332 | 0.9345 | 0.9372 | 0.9389 | 0.94 | 0.941 | 0.942
Energy Savings
Part Density vs. Oven Temperature

## Slide 21
Chart: Part Density vs. PIAT
| 148 | 159 | 172 | 185 | 190 | 210 | 220
N-307 | 0.9276 | 0.929 | 0.931 | 0.936 | 0.937 | 0.939 | 0.9395
Evolve N-307 | 0.9332 | 0.9345 | 0.9372 | 0.9389 | 0.94 | 0.941 | 0.942
Energy Savings
Part Density vs. Oven Temperature

## Slide 22
ARM Impact Strength
Chart: Cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21
N-307 | 0 | 0 | 0 | 60 | 78 | 65 | 75 | 66 | 77 | 80 | 90 | 100 | 110 | 99 | 101 | 0

## Slide 23
Chart: Cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21
N-307 | 0 | 0 | 0 | 60 | 78 | 65 | 75 | 66 | 77 | 80 | 90 | 100 | 110 | 99 | 101 | 0
Evolve N-307 | 0 | 50 | 55 | 59 | 75 | 80 | 90 | 105 | 100 | 106 | 0 | 0 | 0 | 0 | 0
ARM Impact Strength

## Slide 24
Chart: Cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21
N-307 | 0 | 0 | 0 | 60 | 78 | 65 | 75 | 66 | 77 | 80 | 90 | 100 | 110 | 99 | 101 | 0
Evolve N-307 | 0 | 50 | 55 | 59 | 75 | 80 | 90 | 105 | 100 | 106 | 0 | 0 | 0 | 0 | 0
ARM Impact Strength

## Slide 25
Brittleness
Chart: Cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21
N-307 | 100 | 100 | 100 | 33 | 33 | 22 | 28 | 25 | 0 | 0 | 0 | 0 | 0 | 0 | 100

## Slide 26
Brittleness
Chart: Cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21
N-307 | 100 | 100 | 100 | 33 | 33 | 22 | 28 | 25 | 0 | 0 | 0 | 0 | 0 | 0 | 100
Evolve N-307 | 100 | 100 | 100 | 60 | 40 | 0 | 0 | 0 | 0 | 0 | 0 | 100 | 100 | 100 | 100

## Slide 27
Brittleness
Chart: Cook time (min)
| 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21
N-307 | 100 | 100 | 100 | 33 | 33 | 22 | 28 | 25 | 0 | 0 | 0 | 0 | 0 | 0 | 100
Evolve N-307 | 100 | 100 | 100 | 60 | 40 | 0 | 0 | 0 | 0 | 0 | 0 | 100 | 100 | 100 | 100

## Slide 28
Surface Porosity Assessment
Standard Grade Evolve® Grade

## Slide 29
Cross-Section Assessment
Standard Grade Evolve® Grade

## Slide 30
  10-20% reduction in overall cycle time
  potentially increase production output
  Energy savings by 10-20% reduction in gas consumption
  Lower CO2 emission
  Reduction in the number of pinholes, leading to improved part quality
EVOLVE® - Benefits

## Slide 31
Evolve® Technology can:
    Reduce cycle times​
    Increase productivity
    Reduce gas consumption​
    Reduce CO2 emissions
    Reduce Porosity/Pinholes
    Maintain material properties at lower energy input
    Be applied in the entire range of PE and PP grades by MATRIX POLYMERS
Summary

## Slide 32
THANK YOU!
matrixpolymers.com
Dharana Jayawardane
Technical Manager
dharana.jayawardane@matrixpolymers.com
+ 44 7719 910 672